PART 1 – GENERAL

1.1	SUMMARY OF PRODUCT

- EchoFelt Slats manufactured with 100% recyclable polyester fiber without chemical binders. Using 60% recycled materials.

  - SUBMITTALS

- Shop Drawings: Show fabrication and installation details for acoustic slats, including plans, elevations, sections, details and attachment to other work.

- Submittals:  Furnish samples, showing manufacture full range of colors, texture and patterns available for each type of acoustic product specified.

- Qualification Data: For firms specified in “Quality Assurance” Article to demonstrate their capabilities and experience.

- Product Certificates: Signed by manufacturer certifying that the products furnished comply with requirements.

  - QUALITY ASSURANCE

- Manufacturer and Installer Qualifications: Manufacturer and Installer shall have a minimum of 5 years experience in producing and installing specified products and shall furnish supporting documentation showing completed jobs of approximately the same size and scope.

  - DELIVERY, STORAGE, AND HANDLING

- Protect acoustic panels from water, rain, and/or snow when shipping/handling.

- DO NOT drag slats across surfaces as panel damage/soiling can occur.

- 2 people are to carry panels 1200mmx1200mm in size and larger.

- Only install acoustic slats when building is enclosed and HVAC is operational.

- Do not install acoustical slats until wet work is complete and dry.

- Install panels after painting and flooring is completed and/or installed.

PART 2 – PRODUCTS

2.1	PANELS, GENERAL

- The manufacturer’s acoustic panels shall be made with high density (192 kg/m3//12.0 lb/ft3) 100% recyclable polyester fiber without chemical binders.

- Product Model: Echotrol™ EchoFelt Slats

Western Noise Control

T: (800) 661-7241   |   E: info@acousticsolutions.com

- Parent Material Thickness: 12mm (1/2”)

- Slat Depth: 50mm (standard)  |  150mm

- Standard Slat Spacing: 22mm (7/8”)

- Standard Configuration: 24”x96”x2”

- Noise Reduction Coefficient:  50mm Depth=0.75   |  150mm Depth=0.85

- Slat Panel Width: Up to 1200 mm (48”)  - nominal size

- Slat Panel Length: Up to 2440 mm (96”) - nominal size

- Product Options: Custom Slat Spacing Options Available

2.2	CONSTRUCTION

- The acoustic panel product shall be supplied in widths and lengths as indicated.

2.3	MOUNTING

A.	Mounting Accessories: Manufacturer’s standard accessories for securely mounting panels of type and size indicated. Manufacturer's standard hardware will vary by application, if used as a baffle, panel or cloud.

2.4	ACOUSTIC PERFORMANCE

Sound Absorption: Per ASTM C–423 Type A Mounting

50mm Cavity Thick Sound Absorption Coefficient per Octave Band Center Frequency

125Hz	250Hz	500Hz	1000Hz	2000Hz	4000Hz		NRC

0.16	0.38	.75	0.97	0.91	0.89		0.75*

150mm Cavity Thick Sound Absorption Coefficient per Octave Band Center Frequency

125Hz	250Hz	500Hz	1000Hz	2000Hz	4000Hz		NRC

0.37	0.68	0.98	0.81	0.87	0.90		0.85*

*Note:	Average NRC is based on the 250,500, 1000, and 2000 Hz

frequency bands and rounded to nearest multiple of 0.05

2.5	SURFACE BURNING CHARACTERISTICS

- All components pass flame spread and smoke development tests for ASTM E84 Class 1/A.

PART 3 – EXECUTION

  - INSTALLATION

- Install acoustic slats in locations indicated and in alignment with other panels.   Comply with manufacturer’s written instructions for installation of panels using type of mounting accessories as recommended by manufacturer.

  - CLEANING

- After completion of installation of slats, remove dust and other foreign material with a horsehair duster brush mounted on a vacuum cleaner. A damp cloth with mild detergent and warm water or foam/pure water-free solvents can also be used for heavier soiling BUT an inconspicuous section on the side of the panel should be tested beforehand when “wetting” the panel with anything.

END OF SECTION