PART 1 – GENERAL

1.1	SUMMARY OF PRODUCT

- Acoustic Panels manufactured with formaldehyde-free high density acoustic insulation that meets CGSB 51-GP-10M and is GREENGUARD Gold Certified.

  - SUBMITTALS

- Shop Drawings: Show fabrication and installation details for acoustic panels, including plans, elevations, sections, details and attachment to other work.

- Submittals:  Furnish samples, showing manufacture full range of colors, texture and patterns available for each type of acoustic product specified.

- Qualification Data: For firms specified in “Quality Assurance” Article to demonstrate their capabilities and experience.

- Product Certificates: Signed by manufacturer certifying that the products furnished comply with requirements.

  - QUALITY ASSURANCE

- Manufacturer and Installer Qualifications: Manufacturer and Installer shall have a minimum of 5 years experience in producing and installing specified products and shall furnish supporting documentation showing completed jobs of approximately the same size and scope.

  - DELIVERY, STORAGE, AND HANDLING

- Protect acoustic panels from water, rain, and/or snow when shipping/handling.

- DO NOT drag panels across surfaces as fabric/panel damage/soiling can occur.

- 2 people are to carry panels 1200mmx1200mm in size and larger.

- Only install acoustic panels when building is enclosed and HVAC is operational.

- Do not install acoustical panels until wet work is complete and dry.

- Install panels after painting and flooring is completed and/or installed.

PART 2 – PRODUCTS

2.1	PANELS, GENERAL

- The manufacturer’s acoustic panels shall be made with high density (96 kg/m3//6.0 lb/ft3) formaldehyde-free smooth fiberglass wrapped with acoustically transparent fabric.

- Product Model: Echotrol™ Acoustic Wall Panel

Western Noise Control

T: (800) 661-7241   |   E: info@acousticsolutions.com

- Facing Materials: Acoustically Transparent Fabrics as per Architect

- Panel Thickness: Nominal 1”, 2”, 3”, and 4” thick panels.

- Noise Reduction Coefficient:  NRC of 0.8 for 1”, NRC of 1.0 for 2”, and NRC of 1.0 for 4” low frequency panels.

- Panel Width: Up to 1200 mm (48”)  - nominal size

- Panel Length: Up to 3040 mm (120”) - nominal size

2.2	CONSTRUCTION

- The acoustic panel product shall be supplied in widths and lengths as indicated.  All edges will be fully wrapped with mounting as indicated.

2.3	MOUNTING

A.	Mounting Accessories: Manufacturer’s standard accessories for securely mounting panels of type and size indicated and complying with the following requirements:

- Engineered steel panel mounting plates to be securely attached to the wall substrate according to manufacturer’s specification and adhesively bonded to the back of panel.  Adhesive/Sealant is also to be applied to backside perimeter of panel.

2.4	ACOUSTIC PERFORMANCE

Sound Absorption: Per ASTM C–423 Type A Mounting

1” Thick Sound Absorption Coefficient per Octave Band Center Frequency

125Hz	250Hz	500Hz	1000Hz	2000Hz	4000Hz		NRC

0.11	0.24	.73	1.03	1.10	0.87		0.80*

2” Thick Sound Absorption Coefficient per Octave Band Center Frequency

125Hz	250Hz	500Hz	1000Hz	2000Hz	4000Hz		NRC

0.29	0.98	1.09	0.96	1.01	0.97		1.0*

4” Thick Sound Absorption Coefficient per Octave Band Center Frequency

125Hz	250Hz	500Hz	1000Hz	2000Hz	4000Hz		NRC

0.89	1.08	1.03	1.0	1.0	0.92		1.0*

*Note:	Average NRC is based on the 250,500, 1000, and 2000 Hz

frequency bands and rounded to nearest multiple of 0.05

2.5	SURFACE BURNING CHARACTERISTICS

- All components pass flame spread and smoke development tests for CAN/ULC S102-M88 and/or ASTM E84 Class 1/A, NFPA 255, and/or NFPA 260 (Class 1).

2.6	AQUATIC ENVIRONMENT CHARACTERISTICS

- Does not accelerate corrosion on steel, copper or aluminum.

- The corrosion rate in mils/yr. will not exceed that of the 1ppm chloride solution.

- Does not promote mold growth.

- Water vapor sorption is less than 5% by weight.

PART 3 – EXECUTION

  - INSTALLATION

- Install acoustic panels in locations indicated and in alignment with other panels.   Comply with manufacturer’s written instructions for installation of panels using type of mounting accessories as recommended by manufacturer.

  - CLEANING

- After completion of installation of panels, remove dust and other foreign material with a horsehair duster brush mounted on a vacuum cleaner. A damp cloth with mild detergent and warm water or foam/pure water-free solvents can also be used for heavier soiling BUT an inconspicuous section on the side of the panel should be tested beforehand when “wetting” the panel/fabric with anything.

END OF SECTION